CSI Specifications

SECTION 06 06 60
KUVIO Wall Tile System

PART 1 - GENERAL

1.1 RELATED DOCUMENTS

A. Drawings and general provisions of the Contract, including General and Supplementary Conditions and other
     Division 1 Specification sections, apply to this Section.

1.2 SUMMARY

A. This Section includes the Kuvio Wall Tile as shown and specified in the described system(s):

1.     Decorative Wall Panels
     2.     Feature Walls
     3.     Headboards

1.3 SUBMITTALS

A. General: Submit the following in accordance with conditions of contact and Division 1 specification section 
     01 33 00 “Submittal Procedures.”

B. Product Data: Indicate product description, fabrication information, and compliance with specified
     performance requirements.

C. Submit material test results or certifications indicating each type of Kuvio Wall Tile complies with the project
     performance requirements.

1.    Test results required are:

a. Compressive Strength (ASTM D1621)  236 psi
	b. Compressive Modulus (ASTM D1621)  5773 psi
	c. Flexural Strength (ASTM D 790)  Minimum 17,000 psi
	d. Flexural Modulus (ASTM D 790)  Minimum 490,000 psi
	e. Tensile Strength (ASTM D1623)  131 psi
	f. Thermal Conductivity* (ASTM C518)  0.222 BTU·in/ft2·h·˚F
	g. Flammability** (ASTM E84)  20 FSI / 450 SDI
	h. Max Continuous Service Temperature  130˚F

*Tested on foam core.
    	**Molded to 12pcf, 1.5 inches thick, full tunnel width and length.

D. Samples for Initial Selection:

1. Submit representative sample(s).
     2. Indicate shape and finish.
     3. Approved samples will be retained as standards for work.

E. Samples for Verification:

1. Submit sample of each shape and finish.

F. Mockups:

1. Build mockups to verify selections made under sample submittals and to demonstrate aesthetic effects.
     2. Approved mockups may become part of the completed work if undisturbed at time of substantial
         completion.

G. Maintenance Data: Submit manufacturer’s care and maintenance data, including care and cleaning
     instructions. Include in Project closeout documents.

1.4 QUALITY ASSURANCE

A. Manufacturer’s Qualifications

1. Manufacturer must demonstrate leadership in the field of dimensional wall tile with patents or similar proof of
     ownership of intellectual property or expertise.

B. Performance Criteria

1. Compressive Strength (ASTM D1621)  236 psi
     2. Compressive Modulus (ASTM D1621)  5773 psi
     3. Flexural Strength (ASTM D 790)  Minimum 17,000 psi
     4. Flexural Modulus (ASTM D 790)  Minimum 490,000 psi
     5. Tensile Strength (ASTM D1623)  131 psi
     6. Thermal Conductivity* (ASTM C518)  0.222 BTU·in/ft2·h·˚F
     7. Flammability** (ASTM E84)  20 FSI / 450 SDI
     8. Max Continuous Service Temperature  130˚F

*Tested on foam core.
     **Molded to 12pcf, 1.5 inches thick, full tunnel width and length.

C. Allowable Tolerances:

1. Flatness: 1/8" maximum deviation over 12"
     2. Thickness: ±10%
     3. Height/Width: ±10%

1.5 DELIVERY, STORAGE, AND HANDLING

A. Deliver no components to project site until areas are ready for installation.

B. Handle materials to prevent damage to finished surfaces and edges.

C. Provide protective coverings to prevent damage or staining following installation for duration of project.

D. Store components fully supported indoors where atmospheric conditions are controlled to avoid temperature
     extremes and exposure to ultraviolet light and moisture.

E. Follow manufacturer’s recommendations for storage and handling.

F. Before installing Kuvio tiles, permit them to reach room temperature (acclimate).

1.6 PROJECT CONDITIONS

A. Environmental Limitations: Do not install Wall Tile until spaces are enclosed and weatherproof, and ambient
     temperatures and humidity conditions are maintained at the levels indicated for Project when occupied for its
     intended use.

1.7 WARRANTY

A. Provide manufacturer’s 1 year warranty against defects in materials. Warranty shall provide material to
     replace, defective materials.

B. The warranty shall not deprive the owner of other rights or remedies the Owner may have under other
     provisions of the Contract Documents, and is in addition to and runs concurrent with other warranties made
     by the Contractor under the requirements of the Contract Documents.

PART 2 - PRODUCTS

2.1 MANUFACTURERS

A. Manufacturer:

1. Lumicor, Inc., Renton, WA, USA / 1-888-LUMICOR / www.lumicor.com

B. Local Sales Representative contact information:

2.2 MATERIALS

A. Material: Kuvio®.

1. Rigid polyurethane foam with an applied finish.
     2. Product Sizes: Varies.
     3. Thickness: All Shapes: Minimum varies, maximum 1.45"
     4. Finishes: Walnut, Dark Elm, Nantucket, Maple, Shadow, Shimmer Ash, Oxide, Titanuim, Copper, Ripstop,
         Concrete
     5. Basis of Design Product: The design of Dimensional Wall Tile is based on patented Kuvio® tiles as provided
          by Lumicor, Inc. Products from other manufacturers must be approved by the Architect or Designer prior to
          bidding in accordance with the Instructions to Bidders and Section 10 60 00 “Product Requirements”.

B. Description:

___________ shape, _____________ finish, _____________ part number, installed per architect’s drawings.

2.3 FABRICATION

A. General: Fabricate Wall Tile to designs and sizes indicated and to comply with indicated standards. Comply
     with manufacturer’s written recommendations for fabrication.

B. Machining: Acceptable means of machining are listed below. Ensure that material is not chipped or warped by
     machining operations.

1. Sawing: Select equipment and blades suitable for type of cut required.
     2. Drilling
     3. Milling: Climb cut where possible.
     4. Routing

C. Laminating: Laminate to substrates indicated using adhesives and techniques recommended by manufacturer.

2.4 MISCELLANEOUS MATERIALS

A. General: Provide products of shape and finish required for application indicated, and with a proven record of
     compatibility with surfaces contacted in installation.

B. Damp cloth and mild detergent. Adhesive: Titebond Fast Grab Adhesive

PART 3 - EXECUTION

3.1 EXAMINATION

A. Examine substrates, areas, and conditions where installation of Wall Tile will occur, with Installer present, for
     compliance with manufacturer’s requirements. Verify that substrates and conditions are satisfactory for
     installation and comply with requirements specified.

3.2 INSTALLATION

A. General: Comply with manufacturer’s written instructions for the installation of Wall Tile. Directions for
     Kuvio® materials can be found at http://www.lumicor.com/products/kuvio.

B. Utilize fasteners, adhesives and bonding agents recommended by manufacturer for type of installation
     indicated.

C. Install components plumb, level and rigid, scribed to adjacent finishes.

3.3 CLEANING AND PROTECTION

A. Protect surfaces from damage until date of substantial completion. Repair work or replace damaged work
     which cannot be repaired to Architect’s satisfaction.

End of Section 06 06 60

PRODUCT DATA SHEET 1: Kuvio Wall Tile

Product: 			[Replace with Shape name]

Finish: 				[Walnut], [Dark Elm], [Nantucket], [Maple], [Shadow], [Shimmer Ash], [Oxide],
				[Titanium], [Copper], [Ripstop], and [Concrete]